Planar CMOS Project

Part 1:

Create a project directory called “planar”, with a sub-directory called “cmos_shallow”.

Copy the input deck “planar_cmos_1.in” from Brightspace into the cmos_shallow directory.

Run the deck to create a set of sequential cross-section structures – examine some to verify that they look like the images captured in the planar integration flow slideset. Compare the images to the simulation code in the input deck as needed to ensure that you understand the process flow.

The deck performs some extractions of physical dimensions of the devices, including measurements of the depth of the p-channel and p-channel source drain extensions, after the extension anneal step.

Modify the deck to add extraction of the junction depths for the deep s/d junctions after the deep-s/d anneal, following the example used for the extension depth extraction. Perform the extractions halfway between the isolation edge and the nitride spacer edge for each device type.  Name the extracted parameters sd_depth_n and sd_depth_p, and echo them to the process results file.  For full credit, set up the extractions so that the location of the cutlines will properly scale to remain halfway between the isolation and the spacers as the user changes the geometrical parameters of the simulation. (Some more examples of scalable extraction code can be found later in the file after the comment “extract final physical dimensions”).

Run the I-V portion of the deck to create the electrical characteristics. (Set run_process to zero and set run_iv_nmos and run_iv_pmos to 1.)  Use Victory Visual to create a graph combining the log of the drain currents versus gate voltage for the linear and saturation characteristics of the nmos and pmos devices (four curves on the plot), like the graph presented in the lecture slideset.

(Note: the following portions of the project do not depend on successfully completing the actions requested in Part 1 – if you need to you can go on and return to these steps at a later time.)

Part 2:

Create another sub-directory called “cmos_deep” under your “planar” directory. Copy the input deck “planar_cmos_deep_1.in” from Brightspace into your cmos_deep directory. Alter the user inputs to make the following changes:

- Increase the isolation trench depth from 35nm to 150nm; increase the angle of the trench sidewall from 85 degrees to 87 degrees

- Increase the isolation width from 30nm to 40nm

- Increase the space from drawn isolation edges to poly edges from 41nm to 46nm

- Introduce a 10nm overlap of the nwell and the pwell masks beyond the center point of the isolation trench (each mask overlaps the centerline by 10nm; they would overlap each other by 20nm – but, of course, they are not applied to the wafer simultaneously).

- Increase the nitride spacer width from 10nm to 11nm

- Increase the well diffusion time from 14 minutes to 45 minutes

- Increase the silicon depth in the simulation from 0.2um to 0.3um

With those changes made, run the deck all the way through to create electrical results.

Part 3:

The trench depth has been increased from 35nm to 150nm in anticipation of adding recessed SiGe in the pmos source and drain regions. The nmos transistor has been adjusted to create a deeper pwell, with the pwell implant divided into a lower-energy portion before the well drive, followed by a higher-energy portion added after the well drive. The well drive has been increased significantly, from 14 minutes to 45 minutes. The pmos nwell and pmos threshold implants have not yet been adjusted.

Create another project sub-directory called “cmos_sige” under the planar directory. Copy your “planar_cmos_deep_1.in” deck with the new user input values into the new sub-directory as “planar_cmos_sige_1.in”, with “output_root” changed from “pcmosd” to “pcmosds”. Set up the new deck to run from the “flash” load point (6), using a load_file from your cmos_deep directory as a starting point (set load file to “../cmos_deep/sv_pcmosd_1_flash”).

Modify the deck to add recessed SiGe to the pmos source and drain regions according to the following directions. (As you modify the process, add structure exports as appropriate to visualize the results of your changes).

- Add a new user-defined geometry parameter called “sige_to_iso_width” with a value of 5nm.

- Immediately after spacer nitride deposition, add a mask step to place resist over the nmos area, so that the pmos spacer can be etched while leaving the nitride over the pwell (so that the nitride will protect the nmos transistor area from the subsequent SiGe processing). Use the nwell mask with 100nm resist and a deltacd value of the sige-to-isolation width plus half the isolation width, minus the well-overlap parameter. (Define the deltacd value using parameters, not absolute values, so that the deltacd will scale properly as the inputs are altered.) With the new “sige_to_iso_width” parameter set to 5nm, this should put the resist edge just over the STI onto the edge of the nwell – this is somewhat artificial – in reality, we would put the resist edge in the middle of the STI and let the STI oxide mask the silicon etch, but that produces retrograde geometry that the simulator does not have a good way to handle. Note: any STI areas encompassed by an nwell (which we have not drawn) would be exposed to the etch, so the silicon etch must be selective to both nitride and oxide – similarly, the SiGe epitaxy must be selective to either dielectric. (Note that this first process change occurs after the “flash” load point.)

- After the spacer etch (which now forms the pmos spacer only), strip the resist added in step “b”.

- Move the nmos s/d implant (with its mask and strip) to occur after the s/d anneal step (a second anneal will be added later – see step “j”).

- After the nitride etch that forms the pmos spacer, perform the pmos s/d implant and anneal (to activate the dopant and minimize transient-enhanced thermal diffusion in during the following SiGe epitaxy) – just use the existing statements for these steps.

- After the anneal, add an etch through the oxide in the pmos s/d areas, using the nitride as a hardmask. (The oxide thickness should be the sum of the variables “t_gox_sac” and “t_ox_poly” – create a dry etch to remove that summed thickness with a 25% over-etch.)

- Next etch the silicon, using the nitride as a hardmask. To avoid unrealistic stresses, it is important to round the corners of the silicon recess – do this with the following statements:

set x_sige_min=0.5*$iso_width+$sige_to_iso_width

set x_sige_max=0.5*$iso_width+$iso_to_poly_width-$t_ox_poly-$t_nit_spacer

etch dry material=silicon thickness=0.06 ref.z=0 between.x=”$x_sige_min,$x_sige_max” \

profile=”(0,0) (0,0.06) (0.02,0.06)” smooth.roundcorners smooth.distance=0.01

The use of “between.x” usually represents an implicit masking step, but here we are just using it because the present implementation of the tools does not handle a user-defined depth profile combined with a complex hardmask shape very well. As mentioned previously, we would be expecting the silicon etch to be selective to both nitride and oxide, so that no further masking is needed. Also note that to optimize the stress transfer to the channel in a real process, we might use a combination of crystal-plane-selective wet-etch to undercut the spacer and shape the recess edges, along with a dry etch to achieve the desired depth.

- Simulate the SiGe selective epitaxy step by depositing SiGe with a thickness of 0.07um (slight raising of our S/D region, since the trench was 0.06um) with a germanium fraction of 28% and in-situ boron doping of 1e20/cm3:

deposit material=SiGe thickness=0.07 dopants=boron dopingvalues=1e20 \

x.comp=0.28 comp.doping=off upto=-0.008

- After the SiGe epitaxy, mask to protect the pmos spacers while etching the nmos spacers – use the pwell mask, but with a negative deltacd to pull the mask back onto the SiGe so that all the nitride will be removed. The deltacd expression is designed to place the nominal mask edge in the center of the SiGe:

deltacd = -1 * ( $well_overlap+0.5*$iso_width+$sige_to_iso_width + \

0.5*($iso_to_poly_width-$t_ox_poly-$t_nit_spacer-$sige_to_iso_width) )

NOTE:  The tool is presently (2025) exhibiting a bug that causes the resist to completely disappear when a deltacd parameter with value more negative than 2nm is applied to the pwell mask.  In order to correct for this, we can generate a new mask (called “pwell_mod”) with the deltacd value incorporated in the mask coordinates.  To accomplish this, insert the following code (after you have computed the deltacd value):

set mask_overlap=0.1

set x_mask_max=$x_max+$mask_overlap

set y_mask_min=-1*$mask_overlap

set y_mask_size=2*$mask_overlap

set x_well2_min=-1*$well_overlap

set well_mask_width=$x_mask_max+$well_overlap

specifymaskpoly mask=”pwell_mod” rect lb=$x_well2_min-$deltacd,$y_mask_min \

size=$well_mask_width+$deltacd,$y_mask_size

Note that the “set” statements are just repeats of code used to create the original pwell mask, included here to avoid issues if the deck is restarted from a load point beyond the original definitions.

After masking using 100nm resist and the pwell_mod mask (with no deltacd in the mask statement, since the new mask was created with the indicated deltacd), replicate the spacer etch to create spacers for the nmos device, prior to the nmos s/d implant (which was relocated in step “d”). Notice that the nitride over-etch will hit the silicon germanium, so some selectivity would be required. Strip the resist after the etch.

- After the (masked) nmos s/d implant and resist strip (previously relocated to this point in the flow), replicate the rapid anneal step to activate the nmos s/d implant.

From this point the existing flow can continue unchanged with oxide strip and silicide formation.

After completing simulation of the process as modified to add pmos s/d SiGe in steps a) through i), run the I-V characterization portion of the deck.

The nmos device has been previously adjusted (and it should maintain approximately the characteristics observed previously in Part 2), but the now-altered pmos device has not yet been adjusted. The addition of the SiGe has greatly increased the pmos s/d depth, which will result in punchthrough, causing severe leakage current in saturation. Verify this behavior by loading the “pcmosds_1_p_sat_vg0.str” file (which should have been created by your electrical simulation), and contouring the silicon to show the hole current (using the “H+ Current Density” contour selection). Capture an image of this output.

Part 4:

Modify the process flow to correct the punchthrough in the p-channel device, with the following constraints:

- Linear p-channel threshold should be in the range of 0.36-0.38V

- The p-channel saturation off-state current (Vd=-1.2V, Vg=0) should be < 1nA/um

- The p-channel linear subthreshold slope should be < 92mV/decade, while the p-channel saturation subthreshold slope should be < 97mV/decade

- The metallurgical pwell-to-nwell junction edge should intersect the isolation somewhere within the flat bottom region of the isolation trench.

- No portion of the pwell closer to the surface than the bottom of the trench can be converted to n-type material; similarly, no portion of the nwell closer to the surface than the bottom of the trench can be converted to p-type material

- The N-channel characteristics should remain unaltered, i.e., Vtlin, Vtsat, Idsat, Idlin within 2% of their starting values, and saturation off-state leakage below 1nA/um

You are free to change any of the implant and drive steps (including adding or subtracting steps), but the gate stack, the poly width, spacer width, isolation width and depth and N-to-P space must remain the same. The i-v parameters, like the workfunctions, the lifetimes, or the contact resistances, cannot be changed. You can increase the step sizes in the voltage ramps temporarily if you like to make the iv characteristic computation faster, but return to the original values to run your final version.

Hint: the targets can be achieved without altering the well drive or the extension, halo, or deep s/d implants.

Submit the following:

- 100pts:  A copy of the pcmos_1_process.results file from Part 1 showing the extracted deep S/D depths, along with your final planar_cmos_1.in deck and an image of the graph of the log of the four overlayed currents versus gate voltage from Part 1.

- 50pts:  Copies of the four electrical results files, pcmosd_1_n_lin.results, pcmosd_1_n_sat.results, pcmosd_1_p_lin.results, pcmosd_1_p_sat.results from Part 2.

- 150pts:  Your planar_cmos_deep_1.in input deck from Part 3, along with an image showing the contours of the saturation punchthrough current.

- 200pts:  Your final input deck from part 4, along with the four associated electrical results files, and an image of your completed structure with the silicon contoured by net doping. In a separate document, please also submit a short paragraph describing the method you pursued to arrive at the result.

This project is worth 500 points in total.